| CHROME MAGNESITE BRICKS |
| --- |
| BRAND | MgO % (Min.) | Cr2O3 % (Min.) | SiO2 % (Max) | CaO % (Max) | A.P. % (Max) | B.D. gm/cc (Min) | C.C.S. Kg/cm2 (Min) | R.U.L. TA0C (Min) |
| ACL-CHMB-1 | 35 | 22 | - | - | 25 | 2.85 | 200 | 1550 |
| ACL-CHMB-2 | 40 | 18 | 6.5 | - | 20 | 2.90 | 250 | 1600 |
| ACL-CHMB-3 | 45 | 30 | 2.0 | 15 | 20 | 2.95 | 300 | 1650 |

Application: The above bricks are used in Open Hearth Furnace, Front & Back walls, Gas Ports, Uptake, Rotary Kiln, Electric Arc Furnace etc.

| CHEMICALLY BONDED BRICKS |
| --- |
| BRAND | MgO % (Min.) | Cr2O3 % (Min.) | SiO2 % (Max) | CaO % (Max) | A.P. % (Max) | B.D. gm/cc (Min) | C.C.S. kg/cm2 | R.U.L. % Ta0C (Min) |
| ACL-MGC-85 | 85 | - | 6.5 | 2.5 | 16 | - | 450 | 1550 |
| ACL-MCC-1 | 60 | 15 | 6.5 | - | 16 | 2.85 | 250 | 1550 |
| ACL-CHMC-1 | 35 | 22 | - | - | 16 | 2.85 | 250 | 1550 |

Application: The above bricks are used in Open Hearth Furnace, Front walls, End walls, Side walls of Electric Arc Furnace

| CHROME BRICKS |
| --- |
| BRAND | MgO % (Min.) | Cr2O3 % (Min.) | SiO2 % (Max) | CaO % (Max) | A.P. % (Max) | B.D. Gm/cc (Min) | C.C.S. Kg/cm2 (Min) | R.U.L. Ta0C (Min) |
| ACL-CHD | - | 40 | - | - | 20 | - | 500 | - |

Application: The above bricks is used in Hearth of Open Hearth Furnace, Soaking Pit, Rolling Mill & where high abrasion resistance at hearth is required.

Note: The data relates to standard size press-able bricks. 
These are subject to variation for bigger press-able and Hand Moulded Shapes.