| FIRE CLAY AND HIGH ALUMINA CASTBLES |
| --- |
| BRAND | AL2O3 % (Min.) | FeO3 % (Max) | Refract oriness (0C) Orton (Min.) | Max Service Temp. (0C) | B.D. After Casting & Drying at 110 oC gm/cc (Min.) | Grain Size (mm) | Water required for Casting | C.C.S. at 110 0C Kg/cm2 (Min) | C.C.S at Service Temp. kg/cm2 (Min) | Thermal Conductivity K.CAL/M/Hr. at 500oC |
| ACL-DENSE-CAST | 36 | 4 | - | 1300 | 2.0 | 0-5 | 16-17 | 400 | 400 | - |
| ACL-CAST-42 | 42-44 | 4 | - | 1400 | 2.0-2.1 | 0-5 | 16 | 200-300 | 150-200 | - |
| ACL-CRETE | 45 | 4 | 1580 | 1400 | 2.1 | 0-5 | 16 | 250 | 200 | - |
| ACL-CRETE-SUPER | 70 | 5 | 1680 | 1450 | 2.5 | 0-5 | 16 | 350 | 450 | - |
| ACL-CAST-1500 | 50 | 1.5 | 1665 | 1500 | 2.1 | 0-5 | 12-14 | 350 | - | - |
| ACL-CAST-1600 | 60 | 1.0 | 1683 | 1600 | 2.2 | 0-5 | 12 | 350 | - | - |
| ACL-CAST-1700 | 80 | 1.5 | 1800 | 1700 | 2.6 | 0-5 | 12 | 550 | - | - |
| ACL-CAST1750 | 90 | 0.8 | 1820 | 1750 | 2.8 | 0-5 | 12 | 600 | - | - |
| INSULATING CASTABLE AND MORTARS |
| ACL-INSUL CAST-7 | - | 8.5 | 7 | 1100 | 0.75-0.85 | 0-5 | 55 | 12-14 | 6-8 | 0.14 |
| ACL-INSUL CAST-9 | - | 6.0 | 8 | 1100 | 0.9-1.0 | 0-5 | 50 | 15-20 | 10-14 | 0.28 |
| ACL-INSUL CAST-11 | - | 3.5 | 14 | 1350 | 1.1-1.25 | 0-5 | 35 | 35-45 | 40-45 | 0.31 |
| ACL-INSUL CAST-13 | - | 3.5 | 16 | 1350 | 1.3-1.45 | 0-5 | 30 | 50-60 | 50-70 | 0.33 |
| ACL-INSUL CAST-15 | - | 3.2 | 16 | 1350 | 1.5-1.6 | 0-5 | 30 | 90-100 | 70-90 | 0.44 |
| ACL-INSUL CAST-11-L1 | - | 1.5 | - | 1350 | 1.1-1.25 | 0-5 | 35 | 45-55 | 50-60 | 0.34 |
| ACL-INSUL CAST-13-L1 | - | 1.5 | - | 1350 | 1.3-1.45 | 0-5 | 30 | 80-100 | 40-50 | 0.40 |
| ACL-INSUL CAST-15-L1 | - | 1.5 | - | 1350 | 1.5-1.6 | 0-5 | 30 | 130-150 | 90-100 | 0.44 |
| ACL-INS-30 Mortar | 30 | 2.0 | 29-30 | 1300 | - | 0-5 | Ceramic setting | - | - | - |
| ACL-INS-40 Mortar | 40 | 1.8 | 32-33 | 1400 | - | 0-5 | -do- | - | - | - |