HIGH ALUMINA BRICKS

| BRAND | AL2O3% (Min.) | Fe2O3% (Max.) | PCEOrton (Min) | A.P. % (Max) | B.D. gm/cc (Min) | C.C.S. Kg/CC (Min) | R.U.L. ta’C (Min) | P.L.C. for 2hrs at(‘C)% (Max) | Cartercteristics & Uses |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ACL-45B | 45 | 2.5 | 33 | 23 | 2.25 | 300 | 1400 | 1450+ -1.0 | High aluminia bricks resistance to alkall and slag attack |
| ACL-50B | 50 | 2.5 | 34 | 23 | 2.3 | 300-400 | 1420 | 1500+-2.0 | High alumina bricks resistance to alkall and stag attack |
| ACL-60B | 60 | 2.5-3.0 | 34-35 | 23 | 2.5 | 400 | 1430 | 1500+-2.0 | H.A.bricks resistance to alkall and slag attack suitable for cement Royary Klin |
| ACL-70B | 70 | 3.0-3.5 | 36 | 23 | 2.6 | 500 | 1450 | 1600+-3.0 | Ladle linning and EAF |
| ACL-70BD | 70 | 2.0-2.5 | 37 | 20-22 | 2.65 | 600-800 | 1480 | 1600+-+1.5 | Spl. brick for burning zone of cement Rotary Kiln,Ladle Lining & EAF |

| ACL-80B | 80 | 3.0 | 37-38 | 23 | 2.7 | 400-600 | 1500 | 1600+-1.5 | -do- |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ACL-80BD | 80 | 2.0-2.5 | 37-38 | 21 | 2.75 | 500-700 | 1520 | 1600+-1.5 | -do- |
| ACL-85-BDC | 80-85 | 1.5 | 38 | 18-20 | 2.8 | 600-800 | 1550 | 1600+-1.5 | For spl. application in Aluminium Industries & Phosphate bonded Brk. |
| ACL-90 | 90+-2 | 2.5 | 38 | 23 | 2.8 | 600 | - | 1600+-2.0 | For Spl. Application in various Industries. |