| LOW CEMENTCASTABLE & ULTRA LOW CEMENT CASTABLE |
| --- |
| BRAND | ACL-CAST-LC-45 | ACL-CAST-LC-60 | ACL-CAST-LC-70 | ACL-CAST-LC-80 | ACL-CAST-LC-90 |
| PHYSICAL PROPERTIES | 1550 | 1600 | 1600 | 1700 | 1700 |
| Maximum Service Temp.0C |  |  |  |  |  |
| Refractioness Orton/0C Min. | 32 (1717) | 36 (1804) | 36 (1820) | 37 (1820) | 37 (1820) |
| Dry Density (gm/cc) Min (110 oC) | 2.3 | 2.6 | 2.7 | 2.9 | 3.05 |
| Cold Crushing Strength (kg/cm2) At 110o C At 800o C At 1100o C At 1500o C At 1550o C | 700 800 900 1000 - | 700 800 900 1000 - | 750 800 900 - 1000 | 800 900 1000 - 1200 | 950 1000 1150 - 1200 |
| P.L.C. % (Max.) At 800o C At 1100o C At 1500o C At 1550o C | +0.2 +0.3 +1.0 - | +0.2 +0.3 +1.0 - | +0.2 +0.3 - +1.0 | +0.2 +0.3 - +0.8 | +0.2 +0.3 - +0.6 |
| % Water Required for Casting | 4.5 - 5.0 | 4.0 - 4.5 | 4.0 – 4.5 | 4.0 – 4.5 | 3.5 – 4.0 |
| Maximum Grain Size (mm) | 6 | 6 | 6 | 6 | 6 |
| CHEMICAL ANALYSIS |
| AL2O3 (%) Min. | 45 | 60 | 70 | 80 | 90 |
| Fe2O3 (%) Max. | 0.85-1.0 | 1.5 | 1.5 | 1.5 | 1.0 |

| ULTRA LOW CEMENT CASTABLE |
| --- |
| BRAND | Max Service Temp. 0C | Refractor iness (Orton) 0C Min. | B.D. gm/cc at 110 oC Min | P.L.C % (Max.) At At At At 1000 1450 1500 oC oC oC oC | C.C.S. kg/cm2 at 110oC | % Water Reqqd. for Casting | AL2O3 % Min. | Fe2O3 % Max. |
| ACL-CAST ULC-45 | 1550 | 32 (1717) | 2.35 | NIL +0.2 +0.3 +0.7 | 375 | 5/6 | 43 | 0.7 |
| ACL-CAST ULC-90 | 1750 | 37 (1820) | 3.05 | NIL NIL +0.4 +0.6 | 450 | 4/5 | 90 | 1.3 |
| ACL-CAST ULC-95 | 1800 | 40 (1900) | 2.9 | +0.2 +0.5 +0.8 +1.0 | 200 | 3.5/4.4 | 92 | 0.5 |

Note: Data represents typical average properties and do not constitute a specification.

Characteristics: Lower apparent porosity after firing , 
Offers better corrosion resistance High abrasion and spalling resistance