| MAG CARBON BRICKS |
| --- |
| BRAND | MgO % In DBM | Fixed Carbon % (Min) | A.P. % (Max) | B.D. gm/cc (Min) | C.C.S. kg/cm2 (Min) | MOR kg/cm2 at R.T. | Hot MOR kg/gm2 at 1400oC (Min) |
| ACL-MCB-S8 Spl | 98 | 8 | 3 | 3.0 | 500 | 150 | 140 |
| ACL-MCB-S12 | 97 | 12 | 5 | 2.95 | 450 | 120 | 100 |
| ACL-MCB-S8 | 97 | 8 | 5 | 3.0 | 500 | 150 | 120 |
| ACL-MCB-S4 | 97 | 4 | 5 | 3.0 | 500 | 150 | 120 |
| ACL-MCB-M87 | 87 | 8 | 8 | 2.85 | 350 | 100 | - |
| ACL-MCB-M92 | 92 | 8 | 6 | 2.95 | 450 | 100 | - |
| ACL-MCB-M90 | 90 | 8 | 7 | 2.90 | 400 | 100 | - |
| ACL-MCB-95 | 95 | 8 | 5 | 2.95 | 450 | 135 | - |

Application: the above bricks are used in Steel Ladle slag level, Metal line & Hot Spot of EAF.

| ALUMINA MAG CARBON BRICKS |
| --- |
| BRAND | AL2O3 % (Min.) | MgO % (Min.) | Fixed Carbon (Max) | A.P. % (Max) | B.D. gm/cc (Min) | C.C.S Kg/cm2 (Max) | MOR Kg/cm2 at R.T. | P.L.C. at 1500oC/Hrs (Max) |
| ACL-AMC-1 | 60 | 15 | 7 | 9 | 2.80 | 400 | 140 | +1.5 |
| ACL-AMC-2 | 72 | 11 | 8 | 6 | 2.95 | 550 | 180 | +1.5 |
| ACL-AMC-3 | 50 | 30 | 8 | 5 | 3.0 | 550 | 180 | +1.5 |

Application: the above bricks are used in Steel Ladle , Metal Zone, Bottom Bricks.

| MAGNESITE ALUMINA BRICKS |
| --- |
| BRAND | MgO % (Min.) | Al2O3 % (Min.) | SiO2 % (Max) | FeO3 % (Max) | CaO % (Max) | A.P. % (Max) | B.D. gm/cc(Min) | C.C.S. kg/cm2 (Min) | R.U.L.TaoC (Min) |
| ACL-MAGL-I | 80 | 8-10 | 1 | 1 | 2 | 21 | 2.90 | 450 | 1700 |
| ACL-MAGL-II | 74 | 20 | 1 | 1 | 2 | 20 | 2.90 | 450 | 1700 |

Application: the above bricks are used for Cement Rotary Kiln.

Note:  The data relates to standard size pressable bricks.  
These are subjects to variation for bigger pressable and Hand  Moulded Shapes.