| SPECIAL PRODUCTS – 1 |
| --- |
| BRAND | Service Temp oC | Al2O3 % (Min.) | Fe2O3 % (Max) | P.L.C. at % oC 2 Hrs . (Max) | B.D. gm/cc (Max.) | A.P. % (Min.) | C.C.S. kg/cm2 (Min.) | Thermal Conductivity on hot face temp. K.Cal/M/hr/oC Max at 600oC at 800oC |
| SHARAD-0.4 | 1260 | 30-40 | 1.0 | 1200+1.0 | 0.45 | 80 | 7 | 0.16 0.17 |
| SHARAD-0.5 | 1300 | 40-50 | 1.0 | 1250+1.0 | 0.55 | 80 | 15 | 0.18 0.20 |
| SHARAD-0.8 | 1440 | 50 | 1.5 | 1400+1.0 | 0.80 | 65 | 40 | 0.28 0.30 |
| SHARAD-60-LBD | 1550 | 60 | 1.0 | 1550+1.0 | 0.85 | 65 | 40 | 0.32 0.35 |
| SPECIAL PRODUCT – II |
| BRAND | Service Temp. oC | Al2O3 % (Min.) | Fe2O.3 % (Max.) | P.L.C at oC 24 hrs. (Max.) | B.D. gm/cc (Max.) | C.C.S. kg/cm2 (Min.) | Thermal Conductivity on hot face temp. Cal/m/hr/oCMax. At 800oC |
| SHARAD-23 | 1250 | 35 | 1.5 | 1250 +1.50 | 0.65 | 20 | 0.29 |
| SHARAD-26 | 1400 | 45 | 2.0 | 1350 +1.00 | 0.90 | 30 | 0.40 |
| SHARAD-29 | 1550 | 60 | 1.0 | 1450 +0.50 | 1.10 | 45 | 0.42 |
| SHARAD-32 | 1750 | 75 | 0.5 | 1500 +0.75 | 1.35 | 40 | 0.49 |
| SHARAD-101 | 1850 | 95 | 0.5 | 1550 +0.50 | 1.45 | 50 - 90 | 1.20 |

| SILICA PRODUCTS |
| --- |
| BRAND | Service Temp. oC | SiO2 % (Min.) | Fe2O3 % (Max.) | P.L.C. at oC % 12 hrs. (Max.) | B.D. gm/cc (Max.) | C.C.S. kg/cm2 (Min.) | Thermal Conductivity on hot face temp. K.Cal/M/hr/oC/Max. |
| SHARAD-SILICA-75 | - | 75 | 2.5 | 850 +1.0 | 1.0 | 25 | At 600 oC - 0.40 |
| SHARAD-SILICA-90 | - | 90 | 1.5 | 850 +1.0 | 1.1 | 30 | At 600 oC - 0.45 |

Note: The data relates to Standard size pressable bricks. These are subject to variation for bigger pressable and Hand Moulded shapes.